## Slide 1: Nano-Materials Characterization
Yoram Shapira, EE Nano-bio-electronics 18.12.01
Growth and
Processing
Characterization
and Analysis
Design and
Modeling
Nano
Systems

## Slide 2: Nano-Materials Characterization

## Slide 3: Nano-Materials Characterization

## Slide 4: Nano-Materials Characterization

## Slide 5
Transmission Electron Microscope
(TEM)

## Slide 6: Nano-Materials Characterization

## Slide 7: Courtesy Yossi LEREAH Transmission Electron Microscope
Electron source: W, LaB6, FEG
Condenser Lenses (Electromagnetic)
Sample
Objective Lens (determine the point resolution)
Post Sample Lenses
Detector: electron- light converter
Chemical analysis: EDS, GIF
Wavelength at 200KV - 0.0025nm

## Slide 8: Nano-Materials Characterization
Bragg’s Law 2dsinq=lL
Courtesy Yossi LEREAH

## Slide 9: Objective Lens The Core of TEM
Back Focal Plane: Diffraction Pattern
Image Plane
Diffraction Contrast: Bright Field or Dark Field by excluding one of the beams (in the back focal plane)
Phase Contrast by including all beams
Courtesy Yossi LEREAH

## Slide 10: Crystallization of Ge:Al (1)
A branched Morphology in Material Science that is relevant to Life Science
Contrast: Mass thickness, Bragg Conditions
Diffraction: Polycrystalline, Preferred orientation
Yossi LEREAH TEL AVIV University

## Slide 11: Yossi LEREAH TEL AVIV University Crystallization of Ge:Al (2)
Phase Contrast reveals the periodicity of the atoms.
The interface is rough down to atomic scale
Courtesy Yossi LEREAH

## Slide 12: Melting of Nano-Particles
Melting temperature depends on the particle size.
Existence of surface melting.
Diffraction Contrast between solid and liquid phases
Yossi LEREAH TEL AVIV University

## Slide 13: Nano-Materials Characterization

## Slide 14: Nano-Materials Characterization
Courtesy Yossi LEREAH

## Slide 15
Scanning Electron Microscope
(SEM)

## Slide 16: Nano-Materials Characterization

## Slide 17: Collected signals in SEM
Sample
Incident beam
Secondary electrons (SE)
Backscattered electrons (BSE)
Cathodoluminescence(CL)
X-rays
Absorbed current
Courtesy Z. Barkay

## Slide 18: Energy distribution of SE and BSE
Courtesy Z. Barkay

## Slide 19: Signal emission from interaction volume
Rp
Courtesy Z. Barkay

## Slide 20: The origin of high SE spatial resolution
High resolution SE(1): 1 nm
Lower resolution SE(2): 0.1-1 mm
Courtesy Z. Barkay

## Slide 21: Composition dependence
E=30keV
Usually   0.1, at 30KeV
=(z)
Courtesy Z. Barkay

## Slide 22: Basic SEM modes of operation - summary
(*) usually sizes of 1cm, dependent on SEM configuration
(**) voltage and Z dependent
Additional modes: Voltage contrast (VC) and EBIC - usually used in devices and p-n junctions.
Courtesy Z. Barkay

## Slide 23
Ant
Human hair
Eye of an ant
Courtesy A. Merson

## Slide 24: Nano-Materials Characterization

## Slide 25: Surface, Atomic number, Element imaging
BSE
Cu
SE
Courtesy Z. Barkay

## Slide 26: Nano-Materials Characterization
Courtesy Z. Barkay

## Slide 27: Nano-Materials Characterization
Courtesy Z. Barkay

## Slide 28: Nano-Materials Characterization

## Slide 29: Atomic mapping and analysis
Cl
Brr
Agr
Courtesy Z. Barkay

## Slide 30: Nano-Materials Characterization
Courtesy CEA

## Slide 31: Nano-Materials Characterization

## Slide 32
Auger Electron Spectroscopy
Nano-Materials Characterization

## Slide 33
Auger process
Courtesy A. Merson

## Slide 35
Courtesy A. Merson

## Slide 36
Auger Emission
a. X-ray fluorescence
b. Auger emission
Courtesy A. Merson

## Slide 39
Courtesy PHI

## Slide 40
Courtesy PHI

## Slide 41: Nano-Materials Characterization
Courtesy PHI

## Slide 42
Courtesy PHI

## Slide 43
Nano-Materials Characterization
Courtesy PHI

## Slide 44: Nano-Materials Characterization
Courtesy PHI

## Slide 45: Nano-Materials Characterization
Courtesy PHI

## Slide 46
X-ray Photo-electron Spectroscopy
Nano-Materials Characterization

## Slide 47: Nano-Materials Characterization

## Slide 48: Nano-Materials Characterization
Courtesy PHI

## Slide 49: Nano-Materials Characterization
Courtesy PHI

## Slide 50: Nano-Materials Characterization
Courtesy PHI

## Slide 51: Nano-Materials Characterization
Courtesy PHI

## Slide 52: Nano-Materials Characterization
Courtesy PHI

## Slide 53: Nano-Materials Characterization
Courtesy PHI

## Slide 54: Nano-Materials Characterization
Courtesy PHI

## Slide 55: Nano-Materials Characterization

## Slide 56
TOF-SIMS
Nano-Materials Characterization

## Slide 57
Courtesy A. Merson

## Slide 58
Courtesy A. Merson

## Slide 59: Nano-Materials Characterization
Courtesy PHI

## Slide 60: Nano-Materials Characterization
Courtesy PHI

## Slide 61
Scanning Tunneling Microscopy
(STM)
Nano-Materials Characterization

## Slide 62
Courtesy A. Merson
I~exp(-2kd)

## Slide 63
Courtesy A. Merson

## Slide 64
Atomic Force Microscopy
(AFM)

## Slide 65
Non-contact mode
Courtesy A. Merson

## Slide 66: Nano-Materials Characterization
Courtesy Y. Rosenwaks

## Slide 67: Nano-Materials Characterization

## Slide 68: Materials Characterization
Courtesy Dr. Z. Barkai

## Slide 69
Courtesy Dr. Z. Barkai

## Slide 70: Nano-Materials Characterization
STM: Si(7x7)

## Slide 71: Nano-Materials Characterization
A superlattice of alternating GaSb (12 ml) and InAs (14 ml) was MBE grown by W. Barvosa-Carter, B. R. Bennett, and L. J. Whitman. Only every-other lattice plane [Sb (reddish) and As (blueish)] is exposed on the (110) surface.

## Slide 72: Materials Characterization

## Slide 73
Iron (on Cu) “Coral”

## Slide 74: Nano-Materials Characterization
Courtesy Z. Barkay

## Slide 75: Nano-Materials Characterization
Courtesy Z. Barkay

## Slide 76
Courtesy Y. Rosenwaks

## Slide 77: Materials Characterization
Courtesy Y. Rosenwaks

## Slide 78: Nano-Materials Characterization
Courtesy Dr. S. Richter

## Slide 79: Materials Characterization
Courtesy Dr. S. Richter

## Slide 80
Courtesy Dr. S. Richter

## Slide 81: Materials Characterization
Courtesy Dr. S. Richter

## Slide 82: Materials Characterization
Courtesy Dr. S. Richter

## Slide 83: Nano-Materials Characterization
Thank you for your attention
Yoram Shapira
Shapira@eng.tau.ac.il